TECHNICAL DATA SHEET

NANOBUILD s.r.o., Na Folimance 2155/15, 12000 Praha, Czechia

Correspondence address, laboratory: Mayerova 1067, 341 01 Horažďovice

Company identification number: 60647965

e-mail: nanobuildinfo@gmail.com, tel: +420 602305209

Product Name:	    Aqueous Dispersion of Few-Layer Graphene 2DD-W

Product Description:	2DD-W is an aqueous dispersion (suspension) of few-layer graphene, containing graphene particles in the form of stacks primarily composed of 3–20 elemental graphene sheets. It is produced using a patented graphite exfoliation method.

Technical parameters:

| Parameter | Unit | Value |
| --- | --- | --- |
| Average lateral particle size | (μm) | 10–30 |
| Average number of graphene layers per particle | (pcs) | 10 |
| Color | - | dark gray to black |
| Dispersion medium | - | water |
| Graphene concentration | (wt. %) | 4 |
| pH | - | 6,8 – 7,2 |
| Carbon content in graphene | (%) | ≥ 98 |
| Specific surface area | (m2/g) | > 25 |

Applications:	This product acts as an activator of matrix strength properties, enhancing thermal and electrical conductivity, impact resistance, and durability in aggressive environments. It can be used for applications such as electromagnetic wave absorption and shielding, structural concrete treatment, protective coatings, adhesives, composite materials, and more.

The dispersion serves as a base for producing materials with specified and controlled properties by introducing colloidal liquids into the suspension and creating complex heterosystems.

Upon agreement with the customer, this suspension can be further modified with other necessary substances and supplied at concentrations of up to 7.2 %.