TECHNICAL DATA SHEET

NANOBUILD s.r.o., Na Folimance 2155/15, 12000 Praha, Czechia

Correspondence address, laboratory: Mayerova 1067, 341 01 Horažďovice

Company identification number: 60647965

e-mail: nanobuildinfo@gmail.com, tel: +420 602305209

Product Name:	    Water-Polymer Dispersion of Few-Layer Graphene 2DD-WPE

Product Description:	2DD-WPE is a composition of an aqueous dispersion of few-layer graphene and liquid polymer, where the particles of few-layer graphene consist mainly of 3-20 sheets of elemental graphene. The product is manufactured using a patented graphite exfoliation method.

Technical parameters:

| Parameter | Unit | Value |
| --- | --- | --- |
| Average lateral particle size | (μm) | 10–30 |
| Average number of graphene layers per particle | (pcs) | 10 |
| Color | - | dark gray to black |
| Dispersion medium | - | water-soluble polymer |
| Graphene concentration | (wt. %) | 2 |
| pH | - | 6,8 – 7,2 |
| Carbon content in graphene | (%) | ≥ 98 |
| Specific surface area | (m2/g) | > 25 |

Applications:	The product is designed to enhance the electrical conductivity of mineral fibers and improve their anti-corrosion properties, particularly resistance to alkalis and acids, by creating a nanostructured coating on the fiber surface. The coating demonstrates high adhesion to mineral fibers and, when applied, increases their abrasion resistance. This material is compatible with all types of water-based primers.

Upon agreement with the customer, the dispersion can be further treated with other required substances.